Spacer

Company: Menlo Systemes

Material/Grade: 7972/Premium/Special

Diameter: 92 mm

Length: 485 mm

Notes

Item is oversized cores to yield the above sizes

Finish: Waterjet or saw cut on all surfaces

Tolerances: +12 mm/-0 on all dimensions

Special CTE Selection: Crossover temperature >=28°C (in einer anderen mail, die ich fand stand: 28-35°C)