Vacuum optics

Windows

Typ: Broadband precision wedged window (https://www.thorlabs.com/newgrouppage9.cfm?objectgroup_id=8430&pn=WW11050-C)

Ordering No.: WW11050-C

Wavelength: 1050 - 1700 nm

Wedge Angle: 30 +/- 10 arcim

Subsrtate: N-BK7 (Datasheet: https://www.thorlabs.com/newgrouppage9.cfm?objectgroup_id=6973&tabname=N-BK7)

Diameter: Ø1“ 25.4 mm +0.0/-0.2mm

Thickness 5.0 mm +/- 0.1mm

Clear Aperture: >= Ø22.86 mm

Surface Flatness: ≤λ/20 Over Central Ø10 mm; ≤λ/10 Over Entire Clear Aperture

Surface Quality: 20-10 Scratch-Dig

Reflectance Over AR Coating Range: R_avg < 0.5% @ 0° AOI

Wavelength [nm]	Reflectance [%]
1580	0,13389
1570	0,12753
1560	0,10307
1550	0,08615
1540	0,07766
1530	0,07079
1520	0,05383
1510	0,06028
1500	0,05612

Auto Cad (2D): ww11050-c-autocadpdf.pdf

Vacuum isolator

Test report scan copy for vacuum compatible isolators: test_report_scan_copy_for_vacuum_compatible_isolators.pdf